AQUAPANEL®  Cement Board SkyLite | Sample specifications

EXTERIOR CEILINGS WITH

METAL SUBSTRUCTURE.

Position  Number / ME	Specification of services	Individual price

Total price

1	 	m2

Ceiling panelling in compliance with ETA-13 / 0608 with cement-bound boards free of cellulose fibre, building material class A1,

non-combustible according DIN 13501, single-layer panelling.

Product AQUAPANEL® Cement Board SkyLite according to ETA-13 / 0608

2	 	m2

Raw ceiling of:

installation height:	 	mm height above floor:	 	m

3	 	m2

Metal substructure based on DIN EN 13964 of at least 0.6 mm galvanised, corrosion-protected steel profiles.

Suspensions with compression-resistant vernier / universal brackets / threaded rods with spacing a =  	mm

Base profile  	with spacing c =  	mm

Support profile: CD 60 x 27 mm with spacing b = 312.5 mm / 300 mm depending on board dimensions

The spacing should be selected according to the stability verifications. Corrosion protection according to DIN EN 13964, table 7 + 8, minimum corrosion protection Class C *.

Suspension height:  	mm

Fix the substructure to the existing raw ceiling with approved fasteners, e.g. Kunkel ceiling pins, type KDM stainless steel A4, MKT ceiling bolts B 6-da, stainless steel or fischer nail anchor FNA II, stainless steel.

4	 	m2

Insulating layer on request:

Insulation thickness:	 	mm

Heat conductivity group:	 	 Fire behaviour:

Brand, Knauf insulation type:

supply as cavity insulation and install joint-tight.

5	 	m2

Install single-layer panelling from:

Fit single-layer AQUAPANEL® Cement Board SkyLite (cement-bound mineral board, non-combustible (A1), free of cellulose fibre) in groups with 3 – 5 mm board spacing, avoiding cross-joints.

Fasten the AQUAPANEL® Cement Board SkyLite to the substructure with AQUAPANEL® Maxi Screws SN 25 (requirements: 25 per board with board size 900 x 1,250 mm). In the case of cuttings, remain ≥ 15 mm from the edge of the board, with screw spacing of ≤ 220 mm.

6	 	m2

Fill board joints and screw heads with AQUAPANEL® SkyLite Joint Filler &

Skim Coating. Insert AQUAPANEL® Tape (10 cm) in the joint area.

7	 	m2	Prime boards with AQUAPANEL® Board Primer (coverage approx. 40 – 60 g /m2).

8	 	m2

Apply on the whole ceiling surface AQUAPANEL® SkyLite Joint Filler &

Skim Coating, d = 4 mm and embed AQUAPANEL® SkyLite Reinforcing Mesh. The mesh should overlap by 10 cm around the edges.