AQUAPANEL® Cement Board Outdoor

Building envelope exterior wall with timber framework F 90-B/ F30-B

Manufacture, delivery and installation of a load-bearing exterior wall with timber framework, F 90-B/ F 30-B, planked with a double layer of AQUAPANEL® Cement Board Outdoor and Knauf Gypsum Board on the exterior and a single layer of Knauf Gypsum Board on the interior, with finished exterior surface. This is a turnkey solution including connections and supplementary services.

# Specification examples

| Item | Quantity / ME | Description of service | Unit cost | Total cost |
| --- | --- | --- | --- | --- |
|  | m2 m2 m2 m2 m2 RM | Wall thickness: 160 mm Wall height: ___________ cm Ceiling connection to: ___________ Floor connection to: ___________ Cavity insulation: ___________ Insulation thickness: ≥ 140 mm Volumetric weight: ≥ 60 kg/m2 Melting point: > 1,000°C Construct furring in the form of a simple wooden sill and beam framework with 60 x 120 mm wooden supports of Pine, minimum grade S10/C24. Spacing between the studs: ≤ 600/625 mm. Supports fastened with two wood beam connectors each at the top and bottom. Fasten sill and beam to the ceiling and floor at intervals of less than 900 mm. Install Knauf Insulation mineral stone wool in the form of cavity insulation with flush joints, anti-slip. Install double-layer exterior facing: Fit 1st layer of Knauf Impregnated Fireboard or alternatively Knauf Gypsum Fibreboard panels 15 mm, in accordance with the manufacturer’s recommendations using suitable clips or nails. Apply AQUAPANEL® Tyvek® Water-Resistive Barrier with overlapping joints of at least 10 cm over the whole of the surface. Fit the 2nd layer of AQUAPANEL® Cement Board Outdoor 12.5 mm (cementitious, mineral-based construction board, non-combustible (A1), free of cellulose fibres) using suitable screws 5 x 70 mm BTI type SPS Driltec ES 5.0 x 70 mm TX 25 for the exterior surfaces with 3 - 5 mm joint width. The spacing between the fasteners is maximum 250 mm. Fill all board joints with AQUAPANEL® Joint Filler – grey and AQUAPANEL® Tape (10 cm). Also fill the screw heads. Coating with exterior finish Supply plaster finishing profile, manufacturer/type ___________ and fit to the end of the façade plinth facing using AQUAPANEL® Exterior Basecoat - white, conforming with the layers. Supply plaster finishing profile, manufacturer/type __________and fit to the corners / edges / reveals of the façade facing using AQUAPANEL® Exterior Basecoat - white, conforming with the layers. |  |  |

AQUAPANEL® Cement Board Outdoor

Building envelope exterior wall with timber framework F 90-B/ F30-B

# Specification examples

| Item | Quantity / ME | Description of service | Unit cost | Total cost |
| --- | --- | --- | --- | --- |
|  | Unit RM m2 m2 m2 m2 | Apply AQUAPANEL® Reinforcing Mesh, 50 x 30 cm, diagonally above and beneath window, door and other openings. Application of AQUAPANEL® Exterior Basecoat - white, in accordance with the manufacturer’s recommendations, including proper smooth and fold-free embedding of the AQUAPANEL® Reinforcing Mesh. Priming of the exterior basecoat using AQUAPANEL® Basecoat Primer. Proper application and structuring of the exterior finish. Texture: horizontally rendered / vertically rendered / circular rendered / graded. Colour white / other colour tint ____________. Supply and install damp course, air sealing insulation manufacturer/type________ as necessary. Fit the interior facing of AQUAPANEL® Cement Board Indoor 12.5 mm, Knauf Fireboard ≥ 12.5 mm or Knauf Gypsum Fibreboard panels ≥ 12.5 mm in accordance with the manufacturer’s recommendations. All work to be carried out in accordance with the manufacturer’s recommendations. |  |  |