AQUAPANEL® Cement Board Outdoor

Building envelope exterior wall with timber framework F30-B

#### Manufacture, delivery and installation of a load-bearing exterior wall with timber framework, F 30-B, faced with a double layer of AQUAPANEL® Cement Board Outdoor and OSB panels, with finished exterior surface. This is a turnkey solution including connections and supplementary services.

# Specification examples

| Item | Quantity ME | Description of service | Unit cost | Total cost |
| --- | --- | --- | --- | --- |
|  | m2 m2 m2 m2 m2 m2 | Wall thickness 195 mm Wall height: _________ cm Ceiling connection to: _____________________________ Floor connection to: _____________________________ Cavity insulation: _____________________________ Insulation thickness: ≥ 140 mm Volumetric weight: ≥ 60 kg/m2 Construct furring in the form of a simple wooden sill and beam framework with 70 x 140 mm wooden supports of Pine, minimum grade S10/C24. Spacing between studs: ≤ 600/625 mm. Supports fastened with two wood beam connectors each at the top and bottom. Fasten sill and beam to the ceiling and floor at intervals of less than 900 mm. Install Knauf Insulation mineral wool 140 mm, > 60 kg/m3, in the form of cavity insulation with flush joints. Install double-layer facing: Fit 1st layer of OSB panels, 15 mm, in accordance with the manufacturer’s guidelines using 40 mm dry wall screws. Expansion joints are to be placed every 15 m and these must be included in the calculation. Apply AQUAPANEL® Tyvek® Water-Resistive Barrier with overlapping joints of at least 10 cm over the whole of the surface. Fit the 2nd layer of AQUAPANEL® Cement Board Outdoor 12.5 mm (cementitious, mineral-based construction board, non-combustible (A1), free of cellulose fibres) using AQUAPANEL® Façade Screws SN 40 with 3 - 5 mm joint width. The spacing between the fasteners is maximum 250 mm. Fill all board joints with AQUAPANEL® Joint Filler – grey and AQUAPANEL® Tape (10 cm). Also fill the screw heads. Expansion joints are to be placed every 15 m and these must be included in the calculation. Fit interior facing of AQUAPANEL® Cement Board Indoor on OSB panel in accordance with the manufacturer’s recommendations. Note: The vertical joints of the opposite facing in the 1st layer are to be arranged such that they are staggered by 600/625 mm. The horizontal joints are to be staggered by at least 300/312.5mm. The second layers are to be fitted to the first layers with the same staggering. See next page for coating with AQUAPANEL® render. All work to be carried out in accordance with the manufacturer’s recommendations. |  |  |

AQUAPANEL® Cement Board Outdoor

Building envelope exterior wall with timber framework F30-B

# Specification examples

| Item | Quantity / ME | Description of service | Unit cost | Total cost |
| --- | --- | --- | --- | --- |
|  | RM RM RM Unit RM m2 m2 | Coating with exterior finish Supply plaster finishing profile, manufacturer/type ___________ and fit to the end of the façade facing plinth using AQUAPANEL® Exterior Basecoat - white, conforming with the layers. Supply plaster finishing profile, manufacturer/type ___________ and fit to the lintel end member of the façade facing using AQUAPANEL® Exterior Basecoat - white, conforming with the layers. Supply plaster finishing profile, manufacturer/type ___________ and fit to the corners / edges / reveals of the façade facing using AQUAPANEL® Exterior Basecoat - white, conforming with the layers. Apply AQUAPANEL® Reinforcing Mesh, 50 x 30 cm, diagonally above and beneath window, door and other openings. Application of AQUAPANEL® Exterior Basecoat - white, in accordance with the manufacturer’s recommendations, including proper smooth and fold-free embedding of the AQUAPANEL® Reinforcing Mesh. Priming of the exterior basecoat using AQUAPANEL® Basecoat Primer. Proper application and structuring of the AQUAPANEL® render. Texture: horizontally rendered / vertically rendered / circular rendered / graded. Colour white / other colour tint ____________. All work to be carried out in accordance with the manufacturer’s recommendations. |  |  |